## Slide 1
Van der Waals forces in nature
H. Peisker et al. Nature Commun. 4, 1661 (2013)
Insects’ adhesive pads
H. Tian et al. : Soft Matter 16, 5599 (2020)
Gecko effect

## Slide 2
Van der Waals crystals
V. Nikolosi, Science 340, 1226419 (2013)

## Slide 3
Graphite is well known for centuries millennia
Graphite paint - 4’000 BC
Marked sheep – 1500 AC
J. Boardman “The Cambridge ancient history”, Vol. 3. P. 31—69 (2008)
https://www.herdy.co.uk

## Slide 4
Crystal & electronic structure
A. W. Hull, Phys. Rev. 10, 661 (1917)
Structure from X-ray diffraction
P. Debije, P. Scherrer, Physikalische Zeitschrift 17, 277 (1916)
G. W. Semenoff Phys. Rev. Lett. 53, 2449 (1984)
Predictions of Dirac cone
+ a number of possible observations & discussions prior to more recent Geim & Novoselovs work

## Slide 5
Making monolayers
25 mm
Mechanical exfoliation
Liquid exfoliation
Chemical vapor deposition (CVD)
Van der Zande, Nature Mater. 12, 554 (2013)
X. Chen Synth. Metals 210, 95 (2015)
Y. Zhang Acc. Chem. Res. 10, 2329 (2013)
A. P. Kauling Adv. Mater. 30, 1803784 (2018)
K. Novoselov, Science 306, 666 (2004)
100 mm

## Slide 6
Electronic structure: graphene vs. graphite
S. Reich, C. Thomsen, and J. Maultzsch, „Carbon Nanotubes: Basic Concepts and
Physical Properties“, Weinheim, Cambridge (2004)
Parabolic bands
Linear dispersion (Dirac cone)
= massless electrons
= electrons with finite effective masses

## Slide 7
Weakly bound layers
As thin as one atom !
Nobel Prize in Physics 2010
"for groundbreaking experiments regarding the two-dimensional material graphene."
How small can crystal dimensions be ?
Graphene
Graphite

## Slide 8
Demonstration of graphene & its properties
Graphene field-effect transistors
Nobel Prize in Physics 2010
"for groundbreaking experiments regarding the two-dimensional material graphene."
K. Novoselov, Science 306, 666 (2004)
K. Novoselov, Nature 438, 197 (2005)
Massless electrons

## Slide 9
Mechanical strength of graphene
“Our research establishes graphene as the strongest material ever measured, some 200 times stronger than structural steel. It would take an elephant, balanced on a pencil, to break through a sheet of graphene the thickness of Saran Wrap.”
Jim Hone, Columbia U. (2008)
C. Lee, Science 321, 386 (2008)

## Slide 10
Graphene “superlatives”
A. Geim / U. Manchester https://slidetodoc.com/some-things-you-might-be-interested-in-knowing-2/
thinnest imaginable material
largest surface-to-weight ratio (~2, 700 m per gram)
strongest material ‘ever measured’
stiffest known material (stiffer than diamond)
most stretchable crystal (up to 20% elastically)
record thermal conductivity (outperforming diamond)
highest current density at room T (106 times of copper)
highest intrinsic mobility (100 times more than in Si)
conducts electricity in the limit of no electrons
lightest charge carriers (zero rest mass)
longest mean free path at room T (micron range)
completely impermeable (even He atoms cannot squeeze through)

## Slide 11
Beyond graphene
C. Hagen, The New Yorker, Dec. 15 (2014)
K. Novoselov, PNAS 102, 10451 (2005)
Conductor
Superconductor
High-temperature superconductor
Semiconductor
Single layers of different classes of electronic materials

## Slide 12
Hundreds of exfoliable van der Waals materials
V. Nikolosi, Science 340, 1226419 (2013)
…and many more
Superconductors
Magnetic materials
Topological insulators
Hybrid perovskites

## Slide 13
Conductivity of solids

## Slide 14
…a few examples
Graphene semimetal
Boron nitride insulator
Transition-metal dichalcogenides semiconductors (VIS)
Black phosphorous semiconductor (NIR)
Chromium triiodide ferromagnet
Metal-halide perovskite hybrid semiconductor
A. Geim & K. Novoselov Nature Mater. 6, 183 (2007)
J. D. Caldwell et al., Nature Rev. 4, 552 (2019)
S. Manzeli et al., Nature Rev. Mater. 2, 17033 (2017)
Y. Xu et al., Nanoscale, 11, 14491 (2019)
X. Jiang et al., Appl. Phys. Rev. 8, 031305 (2021)
L. Mao et al., J. Am. Chem. Soc. 141, 3 (2019)