## Slide 1
Detecting monolayers
“By eye” – optical contrast
R. R. Nair et al. Science 320, 1308 (2008)
Discrete steps with layer number
Z. H. Ni et al. Nano Lett. 7, 2758 (2007)

## Slide 2
Taking advantage of interference
Si
SiO2
300 nm
Graphene / thin layer graphite
r2
r1
r3
t1
t2
Reflected light: result of multi-layer interference
Wavelength of light matters
SiO2 thickness matters
P. Blake et al. Appl. Phys. Lett. 91, 063124 (2007)

## Slide 3
Solving multi-layer interference problem
P. Blake et al. Appl. Phys. Lett. 91, 063124 (2007)
Simple structure – Fresnel equations
transfer matrix method
Steven J. Byrnes arXiv:1603.02720, https://pypi.org/project/tmm/
More complex structures:

## Slide 4
Atomic force microscopy (AFM)
“Making sure it is a monolayer….”
K. Novoselov, Science 306, 666 (2004)
(C) AFM image of single-layer graphene. Colors: dark brown, SiO2 surface; brown-red (central area), 0.8 nm height; yellow-brown (bottom left), 1.2 nm; orange (top left), 2.5 nm. Notice the folded part of the film near the bottom, which exhibits a differential height of 0.4 nm.
https://simple.wikipedia.org/wiki/Atomic_force_microscope#/media/File:AFMsetup.jpg
Graphene
hBN
Y.-J Cho et al., Sci. Rep. 6, 34474 (2016)

## Slide 5
Transmission electron microscopy (TEM)
“Making sure it is a monolayer….”
Electron source
Anode
(acceleration)
Lenses
Sample
Fluorescent screen (detection)
https://www.technologynetworks.com/analysis/articles/sem-vs-tem-331262
K. Kang et al. Nature 520, 656 (2015)
X. Cui et al. Nature Nanotech. 10, 534 (2015)
MoS2
hBN / graphene / MoS2

## Slide 6
Scanning tunneling microscopy (STM)
“Making sure it is a monolayer….”
N. Marturi, «Vision and visual servoing for nanomanipulation and nanocharacterization in scanning electron microscope», thesis (2014)
M. Ugeda et al. Nature Mater. 13, 1092 (2014)

## Slide 7
Atomic force microscopy
( Addendum: AFM can be operated under ambient conditions and have atomic resolution )
K. Pürkhauer et al. ACS Appl. Nano Mater. 2, 2593 (2019)

## Slide 8
Raman spectroscopy
“Confirming monolayers fast”
A. Molina-Sánchez et al. PRB 84, 155413 (2011)
MoS2
Graphene
A. C. Ferrari et al. PRL 97, 187401 (2006)
E0
E0 - Ephonon
Light scattering under phonon emission

## Slide 9
Second harmonic spectroscopy
2 x E0
Y. Li et al. Nano Lett. 13, 3329 (2013)
Monolayer: non-centrosymmetric
Bulk: centrosymmetric