## Slide 1
Atomically-thin semiconductors
Transistors
Light emitters
Lasers
Detectors
Modulators
Photonic devices
Single photon emitters
…
Radisavljevich et al., Nature Nanotech. 6, 149 (2011)
MoS2
S. Manzeli et al., Nature Rev. Mater. 2, 17033 (2017)

## Slide 2
Transition-metal dichalcogenides (TMDCs)
K. Novoselov, PNAS 102, 10451 (2005)
Realized & studied as monolayers in context of graphene
Frindt & Yoffe, Proc. Royal Soc. Lon. 273, 69 (1963)
Evans & Young, Proc. Phys. Soc. 91, 475 (1967)
Wilson & Yoffe, Adv. Phys. 18, 193 (1969)
Beal et al. J. Phys. C. 5, 3540 (1972)
Known for more than 50 years…

## Slide 3
Light emission
Only monolayers emit light efficiently
1L
K. F. Mak et al., PRL 105, 136805 (2010)
Photoluminescence spectra

## Slide 4
Indirect-to-direct bandgap transition
A. Splendiani et al., Nano Lett. 10, 1271 (2010)
1L
2L
4L
Bulk
Indirect transition
Requires large momentum
Optically dark
Direct transition
Requires zero momentum
Optically bright

## Slide 5
Indirect-to-direct bandgap transition
K. F. Mak et al., PRL 105, 136805 (2010)
Lowest PL peak energy
Indirect
Direct
Bulk

## Slide 6
Electronic coupling
A. Kormanyos et al., 2D Mater. 2, 022001 (2015)

## Slide 7
Electronic coupling
A. Kormanyos et al., 2D Mater. 2, 022001 (2015)
K-points (direct transition)
Q & G-points (indirect transition)

## Slide 9
Energy (eV)
Optical absorbance (%)
1.5
2.0
2.5
3.0
0
5
10
15
20
Optical absorption of TMDC monolayers
< 0.6 nm
Monolayer WS2, room temperature
Non-interacting 2D electrons
Evidence of interactions
Y. Li et al., Phys. Rev. B. 90, 205422 (2014)

## Slide 10
x
y
hn
J. Frenkel, Physical Review 37, 17 (1931)
E. F. Gross and N. A. Karrjew, Dokl. Akad. Nauk SSSR 84, 471 (1952)
Dominate optical response
Bound electron-hole pairs
Excitons =
Exciton formation

## Slide 11
Types of excitons
Localized on one molecule
Extend over many lattice sites
(picene crystal)
Tobias Hertel group, University Würzburg
(carbon nanotube)
P. Cudazzo et al., J. Phys. Cond. Mat 27, 113204 (2015)
Frenkel excitons
Wannier-Mott excitons
Molecular solids
Organic crystals
Molecules
Quantum wells / wires
Inorganic semiconductors

## Slide 12
Reduced effective mass
Coulomb interaction potential
Dielectric screening constant
Effective mass approximation
Exciton binding energy
Exciton radius
(solution in 3D)
Homogenous dielectric medium
Hydrogen model for Wannier excitons

## Slide 13
Dielectric screening in matter
Electric field
Electron cloud (-)
Ion core (+)
Effective field in the opposite direction
Coulomb interaction is usually weak in (inorganic) matter
only 1 – 10% compared to vacuum
Exciton binding energies often ~ 10’s of meV

## Slide 14
Measuring excitons & bandgap
Vbias
VB
CB
M. M. Ugeda et al., Nature Mater. 13, 1091 (2014)
Free-particle bandgap Egap
+ exciton absolute energy EX from PL
1L MoSe2
C. Zhang et al., Nano Lett. 14, 2443 (2014)
SiO2
Graphite
Egap – EX
~ 500 ± 100 meV exciton binding energy
Scanning tunneling spectroscopy

## Slide 15
Ground state n = 1
1st excited n = 2
2nd excited n = 3
Ionization continuum n = ∞
Ionization continuum
n = 1
Photon energy
Optical absorption
Binding energy
n = 2
n = 3
…
= Bandgap
1s
2s
3s
= Bandgap
Measuring excitons & bandgap
Exciton spectroscopy

## Slide 16
T. Kazimierczuk et al., Nature 514, 343 (2014)
E. F. Gross and N. A. Karrjew, Dokl. Akad. Nauk SSSR 84, 471 (1952)
Measuring excitons & bandgap
Historical evidence of excitons
Exciton spectroscopy

## Slide 17
Measuring excitons & bandgap
Phys. Rev. Lett. 113, 076802 (2014)
Phys. Rev. Lett. 113, 026803 (2014)
x30
n = 1
2
3
4
5
~ free carrier bandgap
Ground state exciton
Bandgap
Exciton ground state
2D hydrogen model
Exciton binding energy: 320 meV
Reflectance derivative,
Exciton spectroscopy
monolayer WS2

## Slide 18
D. Mathes and R. Hull http://vcsel.mntl.illinois.edu/projects/crvcl/
Quantum wells
Organic blends
A. A. Bakulin et al., Science 335, 1340 (2012)
Heterostructures

## Slide 19
Cui et al., Nature Nano. 10, 534 (2015)
Geim & Grigorieva, Nature 499, 419 (2013)
Van der Waals assembly
Atomically defined interfaces
Twist degree of freedom
Rivera et al., Nature Nano. 13, 1004 (2018)
Van der Waals heterostructures

## Slide 20
J. Kang et al., Appl. Phys. Lett. 102, 012111 (2013)
Interlayer transition
Type II junction
Charge-transfer state
(also labeled)
Interlayer transitions

## Slide 21
Intralayer exciton
Interlayer exciton
1.3
1.4
1.5
1.6
1.7
Energy (eV)
Photoluminescence intensity
WSe2
MoSe2
WSe2/ MoSe2
Top layer
Bottom layer
Heterostructure
P. Rivera et al., Nature Commun. 6, 6242 (2015)
WSe2
MoSe2
Interlayer excitons

## Slide 22
Moiré lattices

## Slide 23
Moiré lattices
Moiré patterns
H. Yu et al., Sci. Adv. 3, e1701696 (2017)
Spatially-varying energies & selection rules

## Slide 24
Electronic & optical excitations in moiré lattices
Xiadong Xu, https://physicsworld.com/a/twistronics-lights-up-with-moire-exciton-experiments/
+ rich physics of correlated electronic states in artificial superlattices